## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Electrodeposition of Metals from Lunar Regolith Dissolved in Reline
Vesna S. Cvetković1, Nataša M. Petrović1, Ksenija Milicevic Neumann2, Bernd Friedrich3, Jovan N. Jovićević1
1Department of Electrochemistry, Institute of Chemistry, Technology and Metallurgy, National Institute of the RS, University of Belgrade, Serbia; v.cvetkovic@ihtm.bg.ac.rs; 2CEOS UG, Munich, Germany; 3IME Process Metallurgy and Metal Recycling, RWTH Aachen University, Intzestrasse 3, 52056 Aachen, Germany
000

## Slide 2
Introduction & Aim
Molten salt electrolysis (MSE) is currently the most widely used approach for obtaining oxygen and high-purity metals from terrestrial materials, and its direct application to lunar regolith — known as the Magma process.
This investigation focuses on the dissolution of lunar regolith in the DESs and determines the reversible (equilibrium) potentials of dissolved metals in ChCl:Urea, as there is no existing data on this topic. The successful recovery of high-purity silica as well as additional valuable metals present in regolith, which could be useful for various extraterrestrial technological and industrial applications.
Processing temperature: DES vs. molten-salt electrolysis
1573–1848 K
Molten salt electrolysis
(Magma process)
Expensive and hazardous for a lunar crew
323–353 K
Deep eutectic solvent
electrolysis (this study)
Recovered metals could support extraterrestrial industrial and technological applications, effectively bootstrapping more complex lunar infrastructure and operations.
Sustained human presence on the Moon requires in situ resource utilization (ISRU) of the metals present in lunar regolith.
https://doi.org/10.3390/aerospace13030223
Image credits: NASA.
Regolith is abundant and accessible and rich in valuable oxides.

## Slide 3
Experimental
Ar
C.E.
W.E.
Thermocouple
R.E.
Ar
Reline + Regolith
LMS1
Supernatant
layer
LMS 1 major oxide composition: SiO₂ (42.81 wt.%), Al₂O₃ (14.13 wt.%), FeOT (7.87 wt.%), MgO (18.89 wt.%), Cr2O3 (0.21 wt.%)
SEM
EDS
XRD
ICP-OES
Au – Working electrode
Pt – Reference electrode
Pt – Counter electrode
343 K – Working temperature

## Slide 4
Results and discussions
LMS-1 was dissolved in freshly prepared reline (ChCl:Urea). ICP–OES analysis revealed selective oxide dissolution, highlighting the potential of reline for selective metal extraction from lunar regolith.
Oxide Solubility Rate in Reline (wt.%) | Al₂O₃ | SiO2 | Cr2O3 | FeOT | MgO
 | 0.40 | 0.98 | 14.6 | 2.27 | 4.10
Equilibrium potentials of dissolved metals (V vs. Pt) | Al | Si | Cr | Fe | Mg
 | EAl = –0.580 | ESi = –0.250 | ECr= –0.144 | EFe= –0.110 | EMg= –1.280
SEM and EDS of Au cathode after electrolysis at cathodic potential of –0.800 V and V –1.250 V vs. Pt for 4 h, from the reline + regolith electrolyte, temperature 343 K.
ICP-OES analysis data of the resulting deposit obtained at V –1.250 V vs. Pt demonstrate that on average 7 % of Si, 20 % of Al, 23 % of Cr and 5 % of Fe were electrodeposited from the resulting electrolyte.

## Slide 5
Conclusions
First report of lunar regolith oxide dissolution in choline-chloride-based DES.
Reline dissolved regolith oxides (extra N–H / C=O donor sites, higher Cl⁻ activity).
Equilibrium potentials predict the deposition sequence: Fe → Cr → Si → Al → Mg.
Potentiostatic electrolysis confirmed selectivity: Si-rich deposit at −0.800 V vs. Pt; Si + Al (with Cr, Fe) at −1.250 V vs. Pt.
Demonstrates a low-temperature, DES-based electrochemical route for selective ISRU metal recovery from lunar regolith.
Acknowledgments Research was supported by the Science Fund of the RS, #Grant No. 270, Applying advanced product intellectual properties and industrialization workflows to innovative fundamental research ideas in the area of rare earth electrochemical recovery – REMEDIS. V.S.C. and N.M.P. acknowledge the financial support from the Ministry of Science, Technological Development and Innovation of the RS (Contract No: 451-03-33/2026-03/200026).