## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Deposition of Dysprosium from Ethaline deep eutectic solvent
Nataša M. Petrović1, Vesna S. Cvetković1, Branislava Vučetić2, Jovan N. Jovićević1
1Department of Electrochemistry, Institute of Chemistry, Technology and Metallurgy, National Institute of the RS, University of Belgrade, Serbia, vukicevic@ihtm.bg.ac.rs
2Faculty of Physics, University of Belgrade, Serbia
000

## Slide 2
Introduction & Aim
NdFeB Permanent Magnets
Nuclear Reactor Control Rods
High neutron absorption cross - section combined with strong resistance to radiation-induced swelling.
Why Dysprosium Matters ?
Wind turbines
HEV and EV traction motors
Electronics / robotics
Dy Electrodeposition: State of the Art
Molten salts
(chlorides / fluorides)
Ionic liquids
(imidazolium, pyrrolidinium)
DES ?
(ethaline)
Why Deep Eutectic Solvents (DES) ?
[+] Advantages
Low toxicity, biodegradable
Good electrochemical window
Low-cost, simple preparation; operates from 50-90 °C
? Open questions for Dy
Dy raises coercivity and thermal stability of Nd-Fe-B permanent magnets at high temperature.
This study focuses on the electrochemical reduction and electrodeposition of Dy from an ethaline (ChCl+EG) + DyCl₃ DES on gold working electrode, a system not previously investigated. The aim is to characterize the electrochemical behavior and deposition mechanism of Dy, providing fundamental insights relevant for the development of sustainable recovery of Dy from secondary resources.

## Slide 3
Experimental
Choline chloride
+
Ar
Thermocouple
Ethylene glycol
C.E.
W.E.
R.E.
Ar
Ethaline + DyCl3
0.1 M DyCl3
W.E.
Au plate – working electrode
C.E.
Glassy carbon – counter electrode
R.E.
Ag wire – reference electrode
Gamry Interface 1010E potentiostat/galvanostat with Echem Analyst software — CV, SWV, and potentiostatic electrodeposition, all at 70 °C under Ar.
70 °C - working temperature
Scanning electron microscopy (SEM)
Energy dispersive X-ray spectroscopy (EDX)
X-ray photoelectron spectroscopy (XPS)
X-ray diffraction (XRD)
Ethaline has lower viscosity than many other DES systems, which is favorable for electrodeposition.
Cyclic and square-wave voltammetry
Potentiostatic deposition
W.E.

## Slide 4
Results and discussions
Element | Dy | Au | O | Cl
Wt.% | 15.0 | 65.3 | 18.8 | 0.9
Au La1
Dy La1
Cl Ka1
O Ka1
Deposition at -0.8V, 1h
XPS analysis

## Slide 5
Conclusions
Conclusions
Acknowledgments: Research was supported by the Science Fund of the RS, #Grant No. 270, Applying advanced product intellectual properties and industrialization workflows to innovative fundamental research ideas in the area of rare earth electrochemical recovery – REMEDIS. V.S.C. and N.M.P. acknowledge the financial support from the Ministry of Science, Technological Development and Innovation of the RS (Contract No: 451-03-33/2026-03/200026).
Dy(III) was successfully electrodeposited for the first time from a choline chloride–ethylene glycol (ChCl  EG, ethaline) deep eutectic solvent onto a gold electrode at 70 °C, establishing a promising low-temperature route for dysprosium recovery from DES-based electrolytes.
Cyclic voltammetric analysis confirmed that the reduction process of Dy(III) to Dy(0) proceeds via irreversible a singlestep, threeelectron transfer process.
The successful formation of metallic Dy was unambiguously supported by complementary XPS and EDX.