## Slide 1
Photocatalytic degradation of 2,5-diphenyl-1,3-oxazole and 2-(4-biphenyl)-5-phenyl-1,3,4-oxadiazole using ZnO nanoflowers
Trajce Trajkov1, Dobrina Ivanova1,Veronika Mihaylova2, Georgi Hadzhichristov3, Nina Kaneva1
1 Laboratory of Nanoparticle Science and Technology, Department of General and Inorganic Chemistry, Faculty of Chemistry and Pharmacy, University of Sofia, 1 James Bourchier Blvd., 1164 Sofia, Bulgaria
2 Department of Analytical chemistry, Faculty of Chemistry and Pharmacy, University of Sofia, 1 James Bourchier Blvd., 1164 Sofia, Bulgaria
3 Laboratory of Optics and and Spectroscopy, Institute Of Solid State Physics, Bulgarian Academy of Sciences, 72, Tzarigradsko Chaussee Blvd., 1784 Sofia, Bulgaria
28th Congress of Chemists and Technologists of Macedonia
23-26 September, 2026, Metropol Lake Resort, Ohrid, Macedonia

## Slide 2: AIMS
Synthesizing 3D-flower like ZnO powders with rare-earth oxides modification.
Characterization of the surface morphology and crystallite size of the ZnO powders by Scanning Electron Microscopy (SEM), Energy-Dispersive X-ray Spectroscopy (EDS), X-ray Diffraction (XRD).
Investigating how the differences in conjugation and heterocyclic functional groups of PPO and PBD affect their photocatalytic degradation.
Comparing the effect of pure and rare-earth modified ZnO.

## Slide 3: PHOTOCATALYSIS
UV/Visible light activates the photocatalyst to break down contaminants;
Excitation of electrons from valence to conductive band
ZnO+hυ= e-CB + h+VB
PPO/PBD + .O2- (OH.) CO2+H2O

## Slide 4: PHOTOCATALYST AND CONTAMINANTS
Pristine ZnO | Modified ZnO | 2,5-diphenyl-1,3-oxazole (PPO)
Advantages: Low cost; Non-toxicity; Strong UV absorbtion; High electron mobility Disadvantages: Rapid electron-hole recombination; photocorrosion | Modification with rare-earth oxides: ZnO/Gd2O3 ZnO/Sm2O3 ZnO/Eu2O3 Improved charge carrier separation; Suppress recombination(4f electronic configuration) | 
 |  | 2-(4-biphenyl)-5-phenyl-1,3,4-oxadiazole (PBD)

## Slide 5: X-RAY DIFFRACTION
Figure 1. XRD scans for the synthesized pure ZnO and rare-earth modified ZnO powders.
Table 1. Crystallite size and optical band gap calculated for pure and rare-earth modified ZnO nanoflower photocatalysts.

## Slide 6: SCANNING ELECTRON MICROSCOPY
Figure 2. SEM images (along with real image scale) for the studied hierarchical flower-like microstructures of pristine and rare-earth-modified ZnO photocatalysts: (a) ZnO; (b) ZnO/Gd2O3; (c) ZnO/Sm2O3, and (d) ZnO/Eu2O3.

## Slide 7: ENERGY-DISPERSIVE SPECTROSCOPY
Figure 3. EDS spectra of pure ZnO (a) and ZnO modified with Gd2O3 (b); Sm2O3 (c); Eu2O3 (d)

## Slide 8: PHOTOCATALYTIC DEGRADATION OF PBD
Figure 4. UV–Vis absorption spectra during the photocatalytic degradation of PBD under UV irradiation using pure (a) and rare earth-modified ZnO photocatalysts ((b) ZnO/Gd2O3, (c) ZnO/Sm2O3, and (d) ZnO/Eu2O3

## Slide 9
PHOTOCATALYTIC DEGRADATION OF PPO
Figure 5. UV–Vis absorption spectra of PPO during photocatalytic degradation under UV irradiation in the presence of pure and rare-earth-modified ZnO nanoflowers: (a) ZnO, (b) ZnO/Gd2O3, (c) ZnO/Sm2O3, and (d) ZnO/Eu2O3.

## Slide 10: KINETIC ANALYSIS
Figure 6. Concentration ratio (C/C0) of PBD (a,b) and PPO (c,d) as a function of UV irradiation time in the presence of pristine and rare-earth-modified ZnO photocatalysts; (b,d) Pseudo-first-order kinetic plots represented as–ln(C0/C) vs irradiation time for the photocatalytic degradation of PBD(b) and PPO(d)

## Slide 11: RADICAL SCAVENGER EXPERIMENT
AA-Ascorbic acid
IPA-Isopropyl alcohol EDTA-2Na-Ethylenediaminetetraacetic acid disodium salt
AA-superoxide radicals IPA-hydroxyl radicals EDTA-2Na-photogenerated holes

## Slide 12: CONCLUSION
This work reports, for the first time, the photocatalytic degradation of the laser dyes/scintillators PPO and PBD using hierarchical rare-earth modified ZnO nanoflowers under UV irradiation within the emission range 350-400nm for 10 minutes. A comparative evaluation of Sm2O3, Eu2O3 and Gd2O3 modified ZnO demonstrates the influence of rare-earth induced modifications of the electronic structure on the resulting photocatalytic performance. Among the investigated materials ZnO/Eu2O3 exhibited the highest activity, achieving nearly complete degradation of PPO 99.5% and 82.4% degradation of PBD within 10min, together with the highest degradation rate and photodegradation quantum efficiency.

## Slide 13
Thank you for your attention!