## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
ROLE OF THE SURFACE MODIFICATION OF COAL IN ENHANCING THE PROPERTIES OF REVERSE OSMOSIS MEMBRANES
Gentiana HASANI-BEKTESHI, Bashkim THAÇI*, Fetah PODVORICA, Arta DYLHASI
Deparment of Chemistry, University of Prishtina,10 000 Prishtinë, Republic of Kosovo
AEC-P28
High-performance reverse osmosis membranes are expected to simultaneously exhibit high solute rejection, elevated water permeability, excellent chemical stability, and strong resistance to compaction, particularly in aqueous separation applications.1 For several decades, aryl diazonium salts have been employed as reagents to modify a wide range of substrates, including carbons, metals, metal oxides (e.g., ZnO, Al₂O₃), nanomaterials, semiconductors, and polymer surfaces, with aryl moieties.
Coal surface modification in aqueous solution was performed as follows: the coal specimens were treated with boiling water under stirring conditions to remove all dissolved materials, i.e. inorganic part, color, etc. The residual coal after filtering was dried at 105oC to constant weight.
The aryl groups strongly bonded in the coal particle surface had a significant impact on the rheology and morphology of the membranes, and these changes have influenced solute separation and solute solvent permeation rate.
The resulting membranes with enhanced hydrophilicity, look promising for improvement of impact resistance, stability and antifouling characteristics.
Chart: Separation (%)
| 94.82 | 93.89 | 86.1 | 84.29 | 67.430000000000007
50 mM DS | 30.16 | 35.3 | 56.2 | 65.12 | 113.17
20 mM DS | 50.82 | 57.14 | 68.99 | 80.03 | 87.43
15 mM DS | 57.48 | 60.24 | 64.23 | 88.41 | 90.39
10 mM DS | 60.86 | 79.89 | 95.89 | 97.53 | 110.5
5 mM DS | 45.85 | 46.9 | 55.64 | 56.38 | 96.82
316K | 30.99 | 46.08 | 47.63 | 70 | 66.7

## Slide 2
Introduction & Aim
High-performance reverse osmosis membranes are expected to simultaneously exhibit high solute rejection, elevated water permeability, excellent chemical stability, and strong resistance to compaction, particularly in aqueous separation applications.1 For several decades, aryl diazonium salts have been employed as reagents to modify a wide range of substrates, including carbons, metals, metal oxides (e.g., ZnO, Al₂O₃), nanomaterials, semiconductors, and polymer surfaces, with aryl moieties.2 The resulting grafted layers have diverse applications, including surface modification of membranes.3
This paper examines the role of aryldiazonium salt concentration in an aqueous acid medium in the chemical grafting of aryl moieties onto the coal surface, which is subsequently used for reverse osmosis (RO) membrane preparation. Coal particle surfaces were modified by chemical reduction of 4-nitrobenzene diazonium salt at different concentrations in an aqueous acid solution. Introducing aryl groups onto the coal surface, and thus into RO membranes, alters their characteristics, as shown by reverse osmosis parameters and SEM images. The resulting membranes showed the best results with coal particles modified with a middle concentration of aryldiazonium salt in aqueous medium with hypophosphoric acid. At an acceptable reverse osmosis salt rejection level (94.55 %) of NaCl-H2O at a concentration of 0.4 g/dm3 as a reference system at 1.76 MPa, the flux was 42.6 L/hm2.

## Slide 3
Experimental
Coal surface modification in aqueous solution was performed as follows: the coal specimens were treated with boiling water under stirring conditions to remove all dissolved materials, i.e., inorganic parts, color, etc. The residual coal after filtering was dried at 105 °C to constant weight. Typically, 8 g of this coal was dispersed in 100 cm3 acetonitrile, and the same volume of aqueous solutions of (H3PO2, H2SO4, HCl, HNO3, and H3PO4 of the same concentration 0.01M), and 5, 10, 15, 20, 50 mM of +N2C6H4NO2BF4-, under stirring at a temperature < 5 °C for 5 h.
Film casting details
Table 1.Film casting details:
Concentration wt%
Casting solution Batches 317 K-1(I, II, III, IV, V)
___________________________________________
Cellulose acetate (E 398-3) 10
Modified Coal 15
Acetone 61,3
Magnesium perchlorate 1,45
Water 12,25
__________________________________________
Conditions of membrane preparation:
Temperature of casting solution: 24oC
Temperature of casting atmosphere: 24oC
Casting in ambient air: (RH-60%)
Solvent evaporation time: zero min.
Duration of film-setting in ice-cold water~0 ºC: 1hr.

## Slide 4
Results and discussions
 | Film type Batches | film no. | Film shrink. temp. oC | A x 10-11 gmol H2O /cm2 s Pa | DAM/kδ 10-4 cm/s | f, solute sep. % | PR g/h | PWR g/h
(batch 317K-1, II) | H3PO2 10mM DS | 1 | 88 | 3.96 | 1.19 | 89.55 | 60.86 | 61.26
 |  | 2 | 85 | 5.24 | 2.84 | 83.21 | 79.89 | 80.94
 | HCl 10mM DS | 1 | 88 | 2.74 | 0.54 | 93.40 | 40.93 | 42.34
 |  | 2 | 85 | 4.28 | 1.56 | 87.28 | 64.83 | 66.23
 | H2SO4 10mM DS | 1 | 88 | 2.85 | 0.67 | 92.23 | 42.99 | 44.07
 |  | 2 | 85 | 3.79 | 1.52 | 86.71 | 57.67 | 58.62
 | HNO3 10mM DS | 1 | 88 | 2.99 | 0.69 | 92.28 | 45.27 | 46.32
 |  | 2 | 85 | 3.35 | 1.20 | 88.23 | 50.79 | 51.82
 | H3PO4 10mM DS | 1 | 88 | 2.69 | 0.67 | 91.85 | 40.62 | 41.50
 |  | 2 | 85 | 3.67 | 1.53 | 86.39 | 55.79 | 56.72
(batch 317K-1, III) | H3PO2 15mM DS | 1 | 88 | 3.75 | 1.01 | 90.78 | 57.48 | 57.92
 |  | 2 | 85 | 4.01 | 1.21 | 89.45 | 60.24 | 61.98
 | HCl 15mM DS | 1 | 88 | 2.71 | 0.68 | 91.90 | 41.25 | 41.89
 |  | 2 | 85 | 3.19 | 1.06 | 89.30 | 49.32 | 50.51
 | H2SO4 15mM DS | 1 | 88 | 2.00 | 3.76 | 94.07 | 30.10 | 31.02
 |  | 2 | 85 | 3.27 | 7.76 | 91.88 | 48.89 | 50.63
 | HNO3 15mM DS | 1 | 88 | 2.52 | 0.54 | 93.08 | 38.33 | 38.98
 |  | 2 | 85 | 2.77 | 0.64 | 92.38 | 41.75 | 42.93
 | H3PO4 15mM DS | 1 | 88 | 2.64 | 0.60 | 92.49 | 39.43 | 40.87
 |  | 2 | 85 | 3.78 | 1.85 | 84.38 | 57.81 | 58.43
(batch 317K-1, IV) | H3PO2 20mM DS | 1 | 88 | 3.34 | 0.52 | 94.55 | 50.82 | 51.69
 |  | 2 | 85 | 3.76 | 0.88 | 91.82 | 57.14 | 58.06
 | HCl 20mM DS | 1 2 | 88 85 | 2.99 4.62 | 0.87 1.55 | 90.58 87.94 | 45.71 69.97 | 46.20 71.38
 | H2SO4 20mM DS | 1 | 88 | 2.49 | 0.59 | 92.39 | 37.89 | 38.54
 |  | 2 | 85 | 2.82 | 0.73 | 91.55 | 42.93 | 43.65
 | HNO3 20mM DS | 1 | 88 | 3.05 | 0.87 | 90.38 | 45.29 | 47.09
 |  | 2 | 85 | 4.39 | 2.57 | 81.05 | 66.80 | 67.95
 | H3PO4 20mM DS | 1 | 88 | 2.04 | 0.34 | 94.67 | 30.93 | 31.59
 |  | 2 | 85 | 3.85 | 1.49 | 87.03 | 58.59 | 59.60
Chart: Separation (%)
| 94.82 | 93.89 | 86.1 | 84.29 | 67.430000000000007
50 mM DS | 88 | 88 | 88 | 85 | 82
20 mM DS | 88 | 85 | 82 | 80 | 80
15 mM DS | 88 | 85 | 83 | 80 | 80
10 mM DS | 88 | 85 | 82 | 82 | 80
5 mM DS | 88 | 88 | 85 | 85 | 80
Chart: System: NaCl-H2O Feed conc.: 0.4g/dm3 Operation press.: 1.76MPa Film area: 11.92cm2 k=45x10-4cm/s
| 94.82 | 93.89 | 86.1 | 84.29 | 67.430000000000007
50 mM DS | 30.16 | 35.3 | 56.2 | 65.12 | 113.17
20 mM DS | 50.82 | 57.14 | 68.99 | 80.03 | 87.43
15 mM DS | 57.48 | 60.24 | 64.23 | 88.41 | 90.39
10 mM DS | 60.86 | 79.89 | 95.89 | 97.53 | 110.5
5 mM DS | 45.85 | 46.9 | 55.64 | 56.38 | 96.82
316K | 30.99 | 46.08 | 47.63 | 70 | 66.7
Chart: System: NaCl-H2O Feed conc.: 0.4g/dm3 Operation press.:1.76MPa Film area:11.92cm2 k=45x10-4cm/s
| 90.02 | 78.069999999999993 | 75.13 | 73.910000000000025
Acetonitrile | 60.01 | 87.47 | 97.08 | 99.91
H3PO2 | 50.82 | 57.14 | 68.99 | 80.03 | 87.43
HCl | 45.71 | 50.18 | 69.97 | 73.22 | 89.54
H2SO4 | 37.89 | 42.93 | 42.37 | 76.16 | 84.57
HNO3 | 45.29 | 60.28 | 66.8 | 72.48 | 107.2
H3PO4 | 30.93 | 35.74 | 58.59 | 79.98 | 97.91

## Slide 5
Conclusions
Spontaneous grafting of aryl diazonium salts on coal surface particles can be achieved in aqueous acid and aprotic solutions at different concentrations of diazonium salt. Best results are obtained with DS concentrations in the range of 10 – 20 mM. This parameter is shown to be an important casting solution constituent for preparation of heterogeneous reverse osmosis membranes.
The aryl groups strongly bonded to the coal particle surface had a significant impact on the rheology and morphology of the membranes, and these changes have influenced solute separation and solute solvent permeation rate. RO membranes made of modified coal in an aqueous solution of hypophosphoric acid have superior characteristics; significant enhancement of flux compared with CA bare coal membranes.
The resulting membranes with enhanced hydrophilicity look promising for improvement of impact resistance, stability, and antifouling characteristics.