## Slide 1: Synthesis of silver nanospirals
Rok Mravljak, Aleš Podgornik
Faculty for Chemistry and Chemical Technology, University of Ljubljana, Slovenia
28th SCTM, 23.9.- 26.9.2026, Ohrid

## Slide 2: Outline
From silver nanoplates (AgNPt) to more complex nanostructures
Silver nanospiral properties
Silver nanospirals formation mechanism

## Slide 3: AgNP – seeds for AgNPt preparation
Mravljak & Podgornik, ACS Omega 8 (2023) 2760–2772

## Slide 4: AgNPt – preparation and properties
Mravljak & Podgornik, ACS Omega 8 (2023) 2760–2772

## Slide 5: AgNPt – preparation and properties
Mravljak & Podgornik, ACS Omega 8 (2023) 2760–2772

## Slide 6: AgNPt – possible formation mechanism
Mravljak & Podgornik, ACS Omega 8 (2023) 2760–2772
What if some strong binding ligands are introduced before H2O2 addition?

## Slide 7: Effect of different ligands on silver nanoparticle morphology added before H2O2 addition
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 8: Effect of initial MPA concentration and pH value on silver nanoparticle morphology after H2O2 addition
Mravljak et al., Comm. Chem. (2025) 8:292; https://doi.org/10.1038/s42004-025-01684-y

## Slide 9: Effect of MPA addition on silver nanoparticle assembly
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 10: Effect of MPA concentration on silver nanoparticle morphology during consecutive H2O2 addition
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 11: Silver nanospirals morphology
Mravljak et al., Comm. Chem. (2025) 8:292; https://doi.org/10.1038/s42004-025-01684-y
Notes: Tukaj razmisleki glede možnega mehanizma – ne more biti klasična spiralna rast, kako razložiti dendritno rast?

## Slide 12: Why is MPA (mercaptopropionic acid) so special?
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y
Contrary to other ligands (including MAA), MPA exhibits two different conformations when adsorbed, depending on its surface density.
This might explain observed morphology. But is this happening during this synthesis?

## Slide 13: Why is MPA (mercaptopropionic acid) so special?
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 14: Possible silver nanospirals formation mechanism
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 15: Possible silver nanospirals formation mechanism
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y
What happens if synthesis is initiated by Ag ions and not AgNP?

## Slide 16: Possible silver nanospirals formation mechanism
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 17: Possible silver nanospirals formation mechanism
Mravljak et al., Comm. Chem. (2025) 8:292;
https://doi.org/10.1038/s42004-025-01684-y

## Slide 18
THANK YOU VERY MUCH FOR YOUR ATTENTION!