## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Multifunctional Cotton Textiles Modified with La-Doped TiO2: Self-Cleaning and Antibacterial Performance
Stefani Petrova1, Evelina Vasileva2, Nina Danchova2, Veselin Petrov2, Albena Bachvarova-Nedelcheva1
e-mail: stefany@svr.igic.bas.bg
1 Institute of General and Inorganic Chemistry, Bulgarian Academy of Sciences, 1113 Sofia, Bulgaria; 2 Faculty of Chemistry and Pharmacy, Sofia University
“St. Kliment Ohridski”, 1164 Sofia, Bulgaria
000

## Slide 2
Introduction & Aim
The increasing demand for multifunctional smart textiles has encouraged the development of functional coatings that provide self-cleaning and antibacterial properties. Titanium dioxide (TiO₂) is a promising photocatalyst due to its high chemical stability, non-toxicity, and excellent photocatalytic activity, while rare-earth doping offers an effective approach to further enhance its performance.
In this study, pure TiO₂ (T) and La-doped TiO₂ containing 2 mol% (T2L) and 5 mol% La (T5L) were synthesized via a sol-gel method and deposited onto cotton fabrics. The coated textiles were characterized to evaluate their physicochemical properties and tested for self-cleaning and antibacterial activity to investigate the effect of lanthanum doping on their functional performance.

## Slide 3
Experimental
La(NO3)3.6H2O
POWDERS
DEPOSITION
х5
COTTONS
Cotton characteristics:
130 g/m2
325 mg
5x5 cm

## Slide 4
Results and discussions
SEM OF TEXTILE MODIFIED WITH T2L
Peak № | Wavenumber (cm−1) | Peak characteristics
1 | 3500–3100 | O–H
2 | 2916 | –CH2 (-R)
3 | 1645 | Adsorbed H2O
4 | 1433 | –CH (bending)
5 | 1314 | –CH (wagging)
6 | 1028 | C–O
7 | 896 | C1–O–C4
XRD Analysis
SELF CLEANING
FTIR - ATR

## Slide 5
Conclusions
pristine cotton
T
T2L
ANTIBACTERIAL PROPERTIES AGAINST Escherichia COLI
T5L
The work is supported by project No. BG16RFPR002-1.014-0014-C01 “Development Program with a Business Plan for the Laboratory Complex of Sofia Tech Park” which is implemented under the “Research, Innovation and Digitalization for Smart Transformation” Program, co-financed by the European Union through the European
Regional Development Fund; The research equipment used was from the distributed research infrastructure INFRAMAT, which was supported by the Bulgarian Ministry of Education and Science under contract.
Acknowledgments
Pure and La-doped TiO₂ powders were successfully synthesized by the sol–gel method and deposited onto cotton fabrics.
XRD and FTIR analyses confirmed the formation of TiO₂ and the successful modification of the cotton substrate.
SEM–EDS mapping demonstrated the presence and distribution of Ti and La on the modified cotton surface
TiO₂-coated cotton exhibited photocatalytic self-cleaning activity toward both Malachite Green and Methylene Blue under UV irradiation.
The modified textiles demonstrated antibacterial activity against Escherichia coli compared with pristine cotton.