## Slide 1
000
Effect of MgO on the luminescent properties of
SiO2-B2O3-Eu2O3 sol-gel glasses
Hristo Lalkovski1, Lyubomir Aleksandrov1, Albena Bachvarova-Nedelcheva1
1 Institute of General and Inorganic Chemistry, Bulgarian Academy of Sciences, Sofia, Bulgaria,
lalkovski@svr.igic.bas.bg

## Slide 2
Introduction & Aim
The sol–gel method is used for synthesis of organic–inorganic hybrid nanomaterials, based on polycondensation and hydrolysis processes occurring at low temperature.
89SiO2/8B2O3/1Eu2O3/1MgO
~17h
Sol–gel method
Preparation method

## Slide 3
Results
XRD
DTA
IR

## Slide 4
Results
UV-Vis
PL spectra analysis

## Slide 5
Conclusions
SiO2 / B2O3 / MgO sol-gel glasses doped with Eu³⁺ were successfully synthesized.
The presence of MgO in the composition reduces the luminescence intensity.
MgO plays an important role for the luminescent properties of the materials.
These findings are important for designing efficient optical materials for applications such as LEDs, lasers, and photonic devices.
Acknowledgments:
The authors are thankful to the “National Center of Excellence Mechatronics and Clean Tecnologies” for the experimental work supported by the European Regional Development Fund under the “Research Innovation and Digitization for Smart Transformation” program 2021–2027. Research equipment of distributed research infrastructure INFRAMAT (part of Bulgarian National roadmap for research infrastructures) supported by the Bulgarian Ministry of Education and Science.
Paper:
  H. Lalkovski, L. Aleksandrov, D. Mutafchieva, A. Bachvarova-Nedelcheva,
  „Sol-gel processing and properties of Eu3+ doped SiO2-B2O3 glasses“,
  J. Univ. Chem. Technol. Metall., (2026)