## Slide 1: Introduction & Aim
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
OBPC (Scientific Section)
Comparative study of two Medical-Grade HDPE Resins (Bormed HE7541PH and Purell ACP6541A) for Pharmaceutical Packaging Applications
Lazar Andreevski 1, Nikola Pavleski 2,
1,2 Quality Control Pharmaceuticals ALKALOID AD Skopje, Blvd. A. Makedonski 12, 1000 Skopje, Republic of Macedonia
OBPC-P20
Medical grade HDPE resins are critical pharmaceutical packaging materials due to their chemical inertness, mechanical strength, low extractibles and leachables profile, and ability to provide consistent protection of drug products throughout their shelf life.
Material and Methods
Description (Bormed™ HE7541-PH, white 8160)
Bormed™ HE7541-PH is a bimodal high density polyethylene intended for evaluation for use in Healthcare applications. Bormed™ HE7541-PH is typically used in articles produced via injection moulding. Typical applications are (caps, closures, shoulders for tubes, containers for tablets, powder or granules) for Medical and Diagnostic devices or Pharmaceutical packaging.
Description (Purell ACP 6541A)
Exceptional organoleptic properties and outstanding balance of stiffness, toughness and environmental stresscracking resistance make Purell ACP6541A appropriate for the production of closures for still mineral and sparkling water, CSD (soft carbonated drinks) and many other types of food and non-food caps and closures (incl. hinge caps) as well as tube shoulders and compression moulding applications. Purell ACP6541A is additionally used in injection moulding applications in the medical and pharmaceutical market after approval is given by LyondellBasell.
Chart: Melt Flow Rate Comparison of two HDPE resins
| BORMED HE 7541 PH | PUREL ACP6541A
Series 1 | 4 | 1.45
Series 2
Column1
Chart: Comparison of Tensile Modulus Values
| BORMED HE 7541PH | PUREL ACP6541A
Series 1 | 1150 | 1100
Column1
Column2
Chart: Comparison of tensile stress at yield
| BORMED HE7541PH | PUREL ACP6541A
Series 1 | 26 | 22
Series 2
Column1
Chart: Comparison of Hardness Shore D
| BORMED HE7541PH | PUREL ACP6541A
Series 1 | 61 | 55
Series 2
Series 3
Results & Discussions
Conclusion
The research objective is to evaluate key mechanical and processing properties of two medical-grade HDPE resins BORMED™ HE7541PH and PURELL ACP6541A. The significantly higher MFR (Melt Flow Rate) of Bormed™ HE7541PH indicates lower melt viscosity and easier processability. PURELL ACP6541A with lower MFR, suggests higher molecular weight providing improved mechanical robustness. Similar tensile modulus values indicate comparable stiffness. Differences in hardness and tensile strength reflect variations in material rigidity and flexibility. Both HDPE resins demonstrate suitability for pharmaceutical packaging applications, but significant differences in melt flow rate and mechanical properties indicate that material substitution should be carefully validated based on processing conditions, performance requirements and regulatory compliance.