## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Meri Sokolovska1, Rola Moussa2, Ljupcho Pejov1, Vlado Lazarov2, Biljana Pejova1
1Institute of Chemistry, Faculty of Natural Sciences and Mathematics,
SS Cyril and Methodius University, Skopje, Macedonia
2School of Physics Engineering and Technology, University of York, York, YO10 5DD, UK
000
STRUCTURE-PROPERTY RELATIONSHIP AND
PLASMON-ENHANCED PHOTOLUMINESCENCE IN
Ag@Ag2O CORE-SHELL NANOPARTICLE THIN FILMS

## Slide 2
Introduction & Aim
Ag@Ag₂O core-shell nanoparticles (NPs) combine the plasmonic properties of metallic silver with the semiconducting properties of silver oxide. This combination offers opportunities for plasmon-enhanced optical processes, sensing, photocatalysis and optoelectronics.
Objective: To synthesize Ag@Ag2O nanoparticle thin films and investigate the relationships between their structure, morphology, optical properties and photoluminescence response.
Key question: How does the Ag core influence the optical and photoluminescence behavior of the Ag2O shell?
Localized surface plasmon resonance (LSPR)
of the Ag core under optical excitation
Semiconducting Ag2O
shell: optical excitation and
generation of charge carriers
Ag@Ag2O core-shell NPs:
Integration of metallic and
semiconducting components

## Slide 3
Experimental
US-assisted synthesis of
Ag@Ag2O NP thin films:
Core-shell morphology
HRTEM:
XRD, SAED:
Crystal structure and
phase identification
AFM:
Surface and
topography analysis
Raman
spectroscopy:
SERS response
UV-Vis
spectroscopy:
LSPR, optical properties
Photoluminescence
spectroscopy:
Photoluminescence
properties
Characterization methods:

## Slide 4
Results and discussions
Structural and morphological characterization
XRD and SAED confirm the
coexistence of metallic Ag
and Ag2O phase.
HRTEM reveals Ag
core surrounded
by an Ag2O shell.
Surface topography
a)
b)
c)
Height AFM images of Ag@Ag2O NP thin films
prepared under identical sonication (25 min)
and different pre-sonication conditions:
a) 5 min; b) 10 min and c) 20 min.
The pronounced LSPR band
progressively red-shifts and
broadens with increasing Ag
core radius (a) and Ag2O shell
thickness (b).
Optical properties
exc. = 340 nm
The enhanced PL intensity, relative to pure Ag2O nanostructures, is
attributed to the coupling between electronic transitions in the Ag2O
shell and the LSPR field generated by the Ag core.
Photoluminescence enhancement
Raman and SERS response
The enhanced Raman response indicate the strong localized
electromagnetic fields generated by Ag core demonstrating
the potential of the Ag@Ag2O NP thin films as SERS substrates.
Sq = 0.78 ± 0.29 nm
Sq = 5.89 ± 2.42 nm
Sq = 34.88 ± 7.73 nm

## Slide 5
Conclusions
Ag@Ag2O NP thin films (with different geometrical parameters of the core and shell) were successfully synthesized.
XRD, SAED, Raman spectroscopy and electron microscopy confirmed the coexistence of metallic Ag and Ag2O and the formation of core-shell nanostructures.
The films exhibit a pronounced Ag-related LSPR and enhanced Raman response, indicating potential for SERS applications.
Ag@Ag2O NP thin films show enhanced photoluminescence compared with pure Ag2O nanostructures, consistent with plasmon-exciton coupling.
The results highlight the potential of Ag@Ag2O nanostructures for plasmon-enhanced photonic and sensing applications.