## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
CO₂ adsorption in a draft-tube spout-fluid bed with a hydraulic barrier
Katarina Šućurović1, Darko Jaćimovski1, Danica Brzić2, Mihal Đuriš1, Zorana Arsenijević1, Dunja Šijaković3, Tatjana Kaluđerović Radoičić2, Nevenka Bošković Vragolović2
1 Institute of Chemistry, Technology and Metallurgy - National Institute of the Republic of Serbia, University of Belgrade, Belgrade, Serbia , 2 Faculty of Technology and Metallurgy, University of Belgrade, Belgrade, Serbia, 3 Innovation Center, Faculty of Technology and Metallurgy, University of Belgrade, Belgrade, Serbia
000

## Slide 2
Introduction & Aim
CO₂-containing
aeration gas
Spouting gas
Hydraulic barrier
Annulus
Draft tube
Spout
Aim
DTSFB with a hydraulic barrier
Suppresses gas bypass
Downward particle flow
Upward particle transport
Clean gas outlet
Objective 1
To investigate CO₂ adsorption in the DTSFB with a hydraulic barrier under previously established optimal hydrodynamic conditions.
Objective 2
To examine the effects of gas flow rate and inlet CO₂ concentration on adsorption performance.
evaluated through
Gas flow rate
Inlet CO₂ concentration
Breakthrough
Temperature
Capacity
Why this configuration for CO2 adsorption?
Potential for continuous adsorption-desorption process
Separated adsorption
and particle transport
The draft tube primarily enables upward particle transport, while the annulus serves as the CO₂ adsorption zone.
Hydraulic barrier suppresses
aeration-gas bypass
This confines CO2 adsorption to the annulus.
Improved gas–solid contact
Sufficient gas residence time and effective adsorbent utilization
Spout
Draft tube
Annulus
Hydraulic barrier
Spouting gas
CO2-containing aeration gas

## Slide 3
Experimental
Experimental setup
Adsorption experiments were performed under previously established optimal hydrodynamic conditions
Reference adsorption experiment
Adsorbents
Gas flow rates
CO₂ flow rate
Inlet CO2 concentration
Zeolite 13X; Zeolite 5A
VA = 30 m³/h; VS = 15 m³/h
VCO₂ = 20 l/min
Cin = 7.2 vol.% CO₂
Variables investigated
Inlet CO₂ concentration
Total annulus gas flow rate
5.1 vol.%
21.4 m³/h
7.2 vol.%
14 vol.%
16.5 m³/h
31.7 m³/h
Selected hydrodynamic conditions
Aeration gas flow rate, VA
Spouting gas flow rate, VS
Distance of the draft tube from the bottom, l
Draft-tube diameter, ddt
Fraction of spouting gas flowing through the tube, xA
30 m³/h
15 m³/h
15 mm
30 mm
0.033

## Slide 4
Results and discussions
ccv
ccv
ccv
Temperature response at optimal conditions
5A showed a slightly higher and broader temperature peak.
Effect of total annulus gas flow rate
Effect of inlet CO₂ concentration
Lower annulus gas flow rate prolonged gas–solid contact time.
ccv
Breakthrough curves at optimal conditions
5A reached the plateau earlier; 13X showed earlier breakthrough.
Higher inlet CO₂ concentration shortened breakthrough and saturation times.

## Slide 5
Conclusions
Quantitative summary of adsorption performance
Breakthrough and saturation times were determined directly from the experimental breakthrough curves; saturation corresponds to the first point of the experimental plateau.
Main conclusions
1
The DTSFB with a hydraulic barrier enabled CO₂ adsorption in the annulus while the draft tube provided particle circulation.
2
Among the tested adsorbents, 5A showed better overall adsorption performance than 13X at the selected operating point, with a higher adsorption capacity and slightly higher ∆Tmax .
3
Increasing inlet CO₂ concentration shortened tb and ts, while increasing both adsorption capacity and ∆Tmax; the highest capacity reached 435.89 mg CO2/g ads.
4
Within the investigated flow-rate range, increasing the total annulus gas flow shortened tb and ts and increased both adsorption capacity and ∆Tmax, with the highest capacity obtained at 31.7 m³/h.
Overall: the system behaves as a promising hybrid gas–solid contactor for CO₂ capture, combining the ordered gas–solid contact of a moving packed bed with the flexibility of circulating-particle operation. This provides a promising basis for future integrated adsorption–regeneration operation.
Optimal hydrodynamic conditions
5A showed slightly delayed breakthrough, higher adsorption capacity, and a slightly higher temperature rise than 13X.
Adsorbent
tb, s
ts, s
ΔTmax, °C
q, mg CO₂/g
13X
311
1546
13.39
278.06
5A
341
1361
13.90
295.86
Effect of inlet CO₂ concentration
Higher inlet CO₂ concentration increased adsorption capacity and ∆Tmax but accelerated saturation.
Cin, vol.%
tb, s
ts, s
ΔTmax, °C
q, mg CO₂/g
5.1
450
1584
12.0
250.86
7.2
341
1361
13.9
295.86
14.0
250
1090
15.8
435.89
Effect of annulus gas flow rate
Increasing the total annulus flow rate increased adsorption capacity and ∆Tmax while reducing breakthrough and saturation times.
Flow, m³/h
tb, s
ts, s
ΔTmax, °C
q, mg CO₂/g
16.5
529
1590
10.5
195.65
21.4
418
1476
12.6
222.83
31.7
341
1361
13.9
295.86