## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Structural and Morphological Evaluation of Geopolymer–PA12
Hybrid Composites
Ljiljana M. Kljajević1, Olivera A. Erić Cekić2, Miloš T. Nenadović1, Nataša N. Mladenović Nikolić1, Snežana S. Nenadović1, Jelena J. Gulicovski1*
1 Vinča Institute of Nuclear Sciences, National Institute of the Republic of Serbia, University of Belgrade, Mike Petrović Alasa 12-14, Vinča, Belgrade, Serbia rocenj@vin.bg.ac.rs
2Innovation Center of Mechanical Engineering Faculty, University of Belgrade, 11000 Belgrade, Serbia
ICTM-P5

## Slide 2
Introduction & Aim
Geopolymers are stronger, more durable, and more eco-friendly than cement, with lower energy use and carbon emissions.
Composites combining geopolymers with polyamide 12 (PA12) and glass beads attract interest for merging inorganic and organic benefits.
Main drawback: geopolymers are brittle, limiting applications needing toughness and impact resistance.
Solution: integrating thermoplastic polymers like PA12, which offers flexibility, low water absorption, and chemical resistance.
PA12 improves mechanical performance, toughness, and elasticity, especially with fillers or reinforcements.
Challenges: incompatibility between hydrophilic geopolymers and hydrophobic PA12, differing processing temperatures, and scalability/cost issues.
This study aims to develop and analyze a novel type of geopolymer composite
by adding polyamide (PA_2200 and PA_3200 GF) to the geopolymer matrix.
AIM
INTRODUCTION

## Slide 3
Experimental
Sample | PA_2200 (%) | PA_3200 GF (%) | GP (%)
GP1_2200 | 10 |  | 90
GP2_2200 | 30 |  | 70
GP3_2200 | 50 |  | 50
GP4_3200 GF |  | 10 | 90
GP5_3200 GF |  | 30 | 70
GP6_3200 GF |  | 50 | 50
Mix design of synthesized samples, GP_2200 and GP_3200 GF composites
Metakaolin
Polyamide 12 (PA12)
Materials
+
+
Composites GP_3200 GF
Methods of characterization
Mineralogical characterization of all samples was conducted using X-ray powder diffraction (XRPD)
Functional groups of the samples were studied by Fourier-Transform Infrared Spectroscopy (FTIR)
Scanning Electron Microscope with Energy Dispersive Spectroscopy (SEM/EDS) was used for analysis of the microstructure of the obtained geopolymer composites.

## Slide 4
Results and discussions
Figure 1. XRD patterns of PA_2200 and PA_3200 GF
Fig.6.. DRIFT spectra of GP_2200 composites (a- GP1_2200; b- GP2_2200; c- GP3_2200)
Fig. 4. XRDP of GP_2200 samples (a)-GP1_2200; b)- GP2_2200; c)- GP3_2200)
Fig. 5. XRDP of GP_3200 GF samples (a)- GP4_3200 GF; b)- GP5_3200 GF; c)- GP4_3200 GF)
Fig. 7. DRIFT spectra of GP_3200 GF samples (a- GP4_3200 GF; b- GP5_3200 GF; c- GP6_3200 GF
Fig. 2. DRIFT spectra of PA_2200 and PA_3200 GF
GP1_2200
GP6_3200
PA_2200
PA_3200 GF
Fig. 3. SEM micrographs of analysed samples

## Slide 5
Conclusions
Geopolymer and PA12 phases remain distinct but interact at their interfaces.
Waste glass can be incorporated into geopolymer systems, though defects and uneven distribution must be controlled.
In the glass bead–modified composite (GP_3200 GF), silicon content increased without major structural changes.
Main challenge: limited compatibility between the inorganic geopolymer matrix and the organic PA12 phase.
Optimizing processing conditions and using compatibilizers or surface treatments may improve interfacial bonding and phase integration.
This study has been supported by the Ministry of Science, Technological Development, and Innovation of the Republic of Serbia, Contract number: 451-03-33/2026-03/ 200017 (through the realization of research themes: 1702603 and 1702605)
Acknowledgement