## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Influence of physical and chemical parameters on the rheological properties of modified acetylated distarch adipate
Darko Jaćimovski1, Dunja Šijaković2, Katarina Šućurović 1 , Mihal Đuriš1, Nevenka Bošković-Vragolović2, Zorana Arsenijević1
1 Institute of Chemistry, Technology and Metallurgy - National Institute of the Republic of Serbia, University of Belgrade, Belgrade, Serbia
2 Faculty of Technology and Metallurgy, University of Belgrade, Belgrade, Serbia
000

## Slide 2
Introduction & Aim
Investigate the rheological properties of acetylated distarch adipate (E1422).
H3C
O
O
H3C
O
HO
O
OH
O
+
O
C
O
C
O
H3C
(CH2)
4
O
C
O
C
O
H3C
base
+
2 CH3COOH
Acetic anhydride
Adipic acid
Adipic acetic anhydride
Acetic acid
Starch
Starch
bridge
Aim
Industrial applications
Investigation into the effects
of different parameters
Industrial applications
Ketchup and Mayonnaise
Salad dressings and chili sauces
Fruit yogurts and sour cream
Ice creams and puddings
Meat and Bakery products
Fruit fillings for baking
Instant soups and ready meals
Cosmetics, bioplastics, adhesives
2

## Slide 3
Experimental
Mixer
pH meter
NaOH pump
NaOH container
pH probe
Water bath
Reactor
Modifier pump

## Slide 4
Results and discussions
Setback (SB)=C-B
Breakdown (BD)=A-B
Good modified starch:
PV
Good cooking viscosity
BD
Cooking stability and
shear resistance
SB
Good textural stability
SB
Low syneresis
Peak Viscosity (PV)
Breakdown (BD)
Setback (SB)
A
B
C
Temperature profile
 | Roquet | exp I | exp II
Adipate groups | 0.121 | 0.123 | 0.125
Acetyl groups | 1.8% | 1.9% | 2.2%
NMR-example
Within legal limits
2.5% acetyl groups
0.135% adipate groups

## Slide 5
Conclusions
Concentration of acetic anhydride and adipic acid:
The influence of:
Modifier preparation temperature:
Reaction temperature:
Modifier preparation time:
Reaction time:
Water content in the starch suspension:
Na2SO4 content:
Stirrer speed:
acetyl groups
adipate groups
PV
BD
SB
PV
BD
SB
adipate groups
acetyl groups
Crucial
TM
Higher consumption of reactants for the same or similar target
TR
The yield increases up to a certain point, after which the reaction reaches equilibrium
tR
The yield increases up to a certain point, after which the reaction reaches equilibrium
tR
The reaction accelerates, but so does the side reaction of hydrolysis, leading to a higher demand for reactants
PV
BD
SB
The presence of Na2SO4 (osmotic regulator) does not have a significant effect in the experimental reactor, whereas a potential impact exists in the industrial reactor.
Slow
Low yield
Fast
Low yield
Optimal
High yield