## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Rietveld Structural Analysis and Electrocatalytic Activity of GdMn0.5M0.5O3 (M = Cr, Fe, Co) Double Perovskites toward Hydroxide Oxidation and Hydrogen Evolution Reactions
a Besarta Cheliku Ramadani a Jeta Sela,b Leon Stojanov,c David Jovanov, c Miha Bukleski,c Arianit A. Reka,b Valentin Mirceskic and Slobotka Aleksovskac*
1 Mother Teresa University, Skopje, North Macedonia2University of Tetovo, Tetovo, North Macedonia, 3 Ss. Cyril and Methodius University, Skopje, North Macedonia
PSSE-P10

## Slide 2
INTRODUCTION
Perovskite oxides have attracted considerable scientific interest due to their structural versatility and remarkable functional properties. Partial substitution of Mn at the B-site with transition-metal ions provides an effective approach for tailoring their crystal structure, lattice distortion, and catalytic behavior.
This study presents the synthesis and comprehensive characterization of GdMn₀.₅M₀.₅O₃ (M = Cr, Fe, Co) perovskites, with particular emphasis on the relationship between B-site composition, structural features, and electrocatalytic performance.

## Slide 5
Conclusions
Single-phase GdMn₀.₅M₀.₅O₃ (M = Cr, Fe, Co) perovskites with orthorhombic Pnma symmetry were successfully synthesized.
B-site substitution significantly influences structural distortion, lattice stability, and microstructure.
The powders exhibit porous nanocrystalline morphologies, followed by densification after annealing at 900 °C.
Local structural distortions strongly affect the electrocatalytic performance.
GdMn₀.₅Co₀.₅O₃ showed the highest activity toward OH⁻ oxidation, while the Co- and Fe-based compounds demonstrated promising HER activity.