## Slide 1
Surface Interaction of Ni based Electrocatalyst with Hydrogen Peroxide
Name: Nabi Ullah
Sep 24, 2026
Part 2
Part 3
Part 4
Part 1
28th C-SCTM
Faculty of Chemistry, University of Lodz, Poland
Part 5

## Slide 2
Outline
Sep 24, 2026
Importance of H2O2
01
02
03
04
Motivation
Catalyst Synthesis
Results and Discussion
05
Acknowledgment

## Slide 3
Importance of H2O2
Part 1
Environment
Security
Physiological
Importance
Textile Paper Pharma Disinfection
Immunity

## Slide 4
Pollution upgradation
Part 1
H2O2  OH*
Environment
Security
Physiological
Importance
Immunity

## Slide 5
Security and Terrorism
Part 1
Environment
Security
Physiological
Importance
Immunity
Notes: Triacetone triperoxide and diacetone diperoxide

## Slide 6
Immunity
Part 1
Environment
Security
Physiological
Importance
Immunity
Notes: Antipathogen

## Slide 7
Physiological role
Part 1
Environment
Security
Physiological
Importance
Immunity

## Slide 8
Detection of H2O2
Part 2
Detection
Mechanism
Electrochemical techniques | CV | SWV | EFS | DSWV | SWV (gas phase)
Linear range, mol L−1 | 1.0 × 10−4 – 1.0 × 10−3 | 2.0 × 10−5 – 1.0 × 10−3 | 2.0 × 10−5 – 2.0 × 10−4 | 2.0 × 10−5 – 1.0 × 10−4 | 7.4× 10−¹² – 3.7 × 10−¹¹
Slope, A mol−1 L | 4.0× 10−6 | 2.6× 10−6 | 4.1× 10−6 | 1.1× 10−5 | 3.3× 10−11
Intercept, A | 4.4× 10−7 | 1.5× 10−7 | 2.9× 10−6 | 4.9× 10−7 | 1.2× 10−12
LOD, mol L−1 | 1.9 × 10−⁵ | 5.2 × 10−⁶ | 5.9 × 10−⁶ | 4.9 × 10−⁶ | 4.1× 10−13
LOQ, mol L−1 | 6.3 × 10−⁵ | 1.7 × 10−⁵ | 2.0 × 10−⁵ | 1.6 × 10−⁵ | 1.4× 10−12
https://doi.org/10.1007/s00604-025-07325-4

## Slide 9
Reaction Mechanism H2O2 reduction
Part 2
Detection
Mechanism
2HO2⁻(ads) ⇆ O2(ads) + 2HO⁻(ads) (1)
O2(ads) + 2e⁻ + H+(aq) → HO2⁻ (ads) (2)
https://doi.org/10.1007/s00604-025-07325-4
H2O2 reduction in absence of O2
H2O2 reduction in Presence of O2
Notes: CE mechanism,

## Slide 10
Catalyst Synthesis
Part 3
Synthesis
Conditions
https://doi.org/10.1007/s11581-025-06856-3

## Slide 11
Reaction/synthesis conditions
Part 3
Synthesis
Conditions
Temperature: 305 K
Substrate: Si wafer (with native SiO2
Substrate rotation: 20 rpm
Ni source angle: 40°
Ni Source distance: 12.5 cm
Base pressure: 4.5 × 10−6 Pa.
Inner atmosphere: Ar and oxygen,
Total pressure: 0.5 Pa.
Oxygen partial pressure: 0.03, 0.04, and 0.05 Pa,
oxygen purity: 99.9995%
https://doi.org/10.1007/s11581-025-06856-3

## Slide 12
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
SEM of Ni/NiO Thin Film (sample 1)

## Slide 13
SEM of Ni/NiO Thin Film (sample 2)
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3

## Slide 14
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
SEM of Ni/NiO Thin Film (sample 3)

## Slide 15
XRD and EDS of Ni/NiO
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
Notes: Adatom motion 44° and 69°

## Slide 16
XPS of Ni/NiO
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
Notes: The peak at 852.6 eV and corresponding peaks at 856.3 and 858.7 eV, confirms the presence of Ni⁰.
853.7 and 855.4 eV, along with corresponding peaks at 860.8, 863.9, and 866.3 eV, indicate the presence of partially oxidized nickel

## Slide 17
Raman of Ni/NiO Thin Films
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
Notes: intense band at 533 cm− 1, the structure with imperfections, and low crystallinity
The very low intensities, compared to the LO band, of the second order transition at 889 and 1064 cm− 1, indicate that probably the structure is amorphous
Another indication for this kind of phase is the complete absence of 2 M magnon band above 1500 cm− 1, which appears in a highly ordered structures.

## Slide 18
Electrochemical H2O2 reduction
at Ni/NiO-modified electrode
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
Notes: −1.64 × 10⁻⁴ A/cm2 at a potential of −0.6 V vs. Ag/AgCl

## Slide 19
DFT Confirmation
Part 4
XRD, EDX
XPS
Electrochem
SEM
Raman
DFT
https://doi.org/10.1007/s11581-025-06856-3
Notes: The average adsorption energies of OH groups on amorphous NiO and crystalline Ni(111) are − 1.86 and − 3.76 eV, respectively.

## Slide 20
Acknowledgment
Part 5
UNIC
objective
Contact
Acknow
VIP
Prof. Valentin Mirceski
Prof. Vladimir Ivanoski
Prof. Denis Music

## Slide 21
UNIC
Part 5
UNIC
Objective
Contact
Acknow
Support
UNIC Alliance
The European University of Cities ​
in Post-Industrial Transition

## Slide 22
UNIC Objective
Part 5
UNIC
Objective
Contact
Acknow
Support
What is UNIC?
UNIC is the European University of Cities in Post-Industrial Transition. It ’s one of over 65 European Universities Alliances, part of an ambitious and flagship EU initiative.
We are an alliance of ten universities based in post-industrial cities with a mission to boost mobility and inclusion for societal impact.
Together, we educate through teaching, research, innovation, and community engagement, towards inclusive societies.

## Slide 23
Part 5
UNIC
objective
Contact
Acknow
Support
Student and staff mobility between partner universities.
Joint research projects involving researchers from different European countries.
Joint and innovative educational programmes.
Virtual mobility and online courses, allowing students to learn with colleagues from other UNIC universities.
Thematic conferences, workshops and international networking.
Collaboration with cities, communities and organisations to create practical solutions to urban and societal challenges.
University of Lodz Support

## Slide 24
Link & Contact
Part 5
UNIC
Objective
Contact
Acknow
Support
www.unic.eu
www.uni.lodz.pl/unic
unic@uni.lodz.pl

## Slide 25
You are welcome to ask Questions