## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
SYNTHESIS AND INVESTIGATION OF La1-xERxMn0.5Fe0.5O3
(x = 0.2 and 0.4) COMPLEX PEROVSKITES
Cvetanka Trajkovska1, Sofija Popovska Blazhevska1, Miha Bukleski1, Iwona Misztalewska-Turkowicz2, Angieszka Z. Wilczewska2, Slobotka Aleksovska1
1 Institute of Chemistry, Faculty of Natural Sciences and Mathematics, Ss. Cyril and Methodius University, Skopje, North Macedonia, cvetanka2000@hotmail.com ,
2 Faculty of Chemistry, University of Bialystok, Bialystok, Poland

## Slide 2
Introduction
Perovskite-type ceramic materials with the general formula ABO3 have attracted considerable attention because of their significant electrical, magnetic, and catalytic properties and their potential future use. Among them, mixed-cation perovskites containing two different lanthanide ions at the A-site and two transition-metal ions at the B-site have attracted particular attention because cation substitution can effectively tune their structural and functional properties. This poster presents the synthesis and characterization of La1-xErxMn0.5Fe0.5O3
(x = 0.2 or 0.4).
Experimental - Synthesis method
sol solution
precursors
(metal nitrates)
evaporation
water
citric acid
ammonia solution
(controlling pH)
Figure 1. Schematic representation of the sol-gel combustion method
viscous gel
combustion
annealing
(900 C°)

## Slide 3
SEM with EDX
PXRD
Intensity / a.u
Figure 2. XRD patterns of La1-xErxMn0.5Fe0.5O3
Results and discussions
Figure 3. SEM picture of La0.8Er0.2Mn0.5Fe0.5O3
Figure 4. SEM picture of La0.6Er0.4Mn0.5Fe0.5O3
Element | Atomic %
O | 55.96667
La | 18.03
Mn | 10.73333
Fe | 11.40667
Er | 3.873333
Table 1. EDX of La0.8Er0.2Mn0.5Fe0.5O3
Table 2. EDX of La0.6Er0.4Mn0.5Fe0.5O3
Element | Atomic %
O | 54.24667
La | 14.33333
Mn | 10.95333
Fe | 12.38
Er | 8.09

## Slide 4
Results and discussions
Raman spectroscopy
FTIR
Figure 6. Mid-IR spectra of La1-xErxMn0.5Fe0.5O3 recorded at room temperature using a spectrum of pure KBr as the background spectrum
Chart: Wavenumber/cm-1
Figure 5. Raman spectra of
La1-xErxMn0.5Fe0.5O3
Figure 7. Far-IR spectra of La1-xErxMn0.5Fe0.5O3 recorded at room temperature using a spectrum of pure PE as the background spectrum

## Slide 5
Conclusions
The studied compounds are new and have not been examined yet. The sol-gel combustion method was shown to be an appropriate method for the synthesis of this type of compound. The XRD patterns confirmed the purity and crystallinity of the obtained powders and implied that
La1-xErxMn0.5Mn0.5O3 are probably cubic. Comparing the recorded XRD patterns with those of the pristine La/Er perovskites indicated that the partial substitution was successful. The IR spectra showed characteristic metal-oxygen stretching and bending modes. The observed Raman spectra suggest the presence of local structural disorder and distortion of the (Mn,Fe)O6 octahedra, due to the Jahn-Teller activity of Mn3+ ions. The provided SEM pictures show that the perovskites consist of nanoparticles with significant porosity between them. EDX analysis indicates that the elemental proportions are close to the target values.
Acknowledgement
Part of the experimental research (SEM with EDX and Raman) presented here was conducted at the BioNanoTech Centre, Faculty of Chemistry, University of Białystok in Białystok, Poland, during an Erasmus+ student mobility.