## Slide 1
28th Congress of SCTM, 23-26 September, Ohrid, Macedonia
Ferrite-based sorbent for efficient removal of Reactive Blue 19 dye
Miloš Kostić, Nena Velinov Georgiev, Slobodan Najdanović, Miljana Radović Vučić, Milica Petrović, Jelena Mitrović, Kristina Filipović
Department of Chemistry, Faculty of Sciences and Mathematics, University of Niš, 18000 Niš, Serbia, e-mail: nena.velinov@yahoo.com, nena.velinov@pmf.edu.rs
Environmental contamination by reactive textile dyes, represents a serious and persistent threat to living organisms. Reactive Blue 19 (RB19) is a stable anionic dye containing electrophilic vinylsulfone groups, which may contribute to its toxic and mutagenic potential. Sorption is widely applied for dye removal from water due to its efficiency, low cost, and simple operation. The zinc–manganese ferrite carbonate was synthesized by coprecipitation. Bach experiments evaluated the influence of pH, dye concentration, contact time, and sorbent dosage on RB19 removal. Sorption mechanisms were analyzed using kinetic and isotherm models.
Introduction & Aim
The co-precipitation process was used for the synthesis of the sorbent. Three solutions were made by individually dissolving iron(III) chloride hexahydrate, zinc chloride, and manganese(II) chloride tetrahydrate in deionized water. Then, all three solutions were mixed together in an Erlenmeyer flask with the addition of a reflux condenser, heated and stirred (80 ◦C and 400 rpm). Slow precipitation was carried out by the dropwise addition of 2.0 mol dm⁻3 NaOH and 1.0 mol dm⁻3 Na2CO3 until the solution reached pH 10.0. The obtained material from this synthesis process was abbreviated as ZnMn–Fe2O4–CO3.
Experimental
Optimal sorption of RB19 was achieved at pH 2 and sorbent dose of 0.25 g/L, yielding a maximal sorption capacity of 1463.1 mg/g. Kinetic and equilibrium studies confirm chemisorption as the dominant mechanism, with Langmuir isotherm fitting indicating a homogeneous sorption surface.
Conclusions
Results and discussion
Effect of contact time and initial RB19 concentration, and Effect of pH on RB19 removal.
Acknowledgement The authors would like to acknowledge financial support from the Ministry of Science, Technological Development and Innovation of the Republic of Serbia (Agreement No 451-03-33/2026-03/200124 and 451-03-34/2026-03/200124)
CE-P5